Wire Rod and Stitch Coupon Limits

| Field | Value |
| --- | --- |
| Document No. | STD-CU-309 |
| Revision | 3.0 |
| Effective Date | 2026-05-30 |
| Author | Evan Brooks, Incoming Quality Engineer |
| Classification | Controlled |

## 1. Purpose

Control oxygen-sensitive wire rod and stitch coupon lots before anneal and microbond evaluation.

## 2. Applicability

Apply to incoming E-Cu58 and stitch-wire coupons; use other standards only when they are more stringent.

## 3. Limits

| Impurity or field | Limit / rule |
| --- | --- |
| Oxygen | 5.0 ppm |
| Sulfur | 6.0 ppm |
| Lead | 7.0 ppm |
| Bismuth | 3.0 ppm |
| Iron | 12.0 ppm |
| Nickel | 5.0 ppm |

## 4. Notes

The oxygen and nickel limits here are intentionally lower than the base material table because wire-draw defects are sensitive to both species.