## Slide 1
QUALIFICATION READOUT
Five lots. One model-derived risk landscape.
01
Configured thresholds
CONDITIONAL ≥ 8
HOLD ≥ 45
LOT A
CU-C101
0
RELEASE
LOT B
CU-WIRE
12
CONDITIONAL
LOT C
CU-HBPLATE
8
CONDITIONAL
LOT D
CU-HBPLATE
88
HOLD
LOT E
CU3SN-ETA
44
CONDITIONAL
8
45
LOT E sits one point below HOLD under the configured score threshold despite a chemistry violation.
CU-JULY-2026-QUAL • 24 JUL 2026 • MODEL-DERIVED VISUAL READOUT
technical_findings_matrix.xlsx · Calculations!O71:P75

## Slide 2
RISK COMPOSITION
The score is the sum of model flags × configured weights.
02
Chemistry 40
Electrical 25
Margin <10 mΩ 15
Exception 8
Literature 5
Catalog 4
LOT A
RELEASE
0
LOT B
CONDITIONAL
8
12
LOT C
CONDITIONAL
8
8
LOT D
HOLD
40
25
15
8
88
LOT E
CONDITIONAL
40
44
LOT D = 40 + 25 + 15 + 8 = 88
LOT B = exception 8 + catalog 4
LOT E = chemistry 40 + catalog 4
CU-JULY-2026-QUAL • 24 JUL 2026 • MODEL-DERIVED VISUAL READOUT
technical_findings_matrix.xlsx · Calculations!C71:O75

## Slide 3
TRACEABLE CALCULATION CHAIN
Only selected protocol matches feed the resistance margin and risk.
03
MEASURED
HB resistivity
1.762 µΩ·cm
GEOMETRY
50 mm × 400 µm
17.8 µm average
SERVICE
85 °C adjustment
α = 0.00393 /°C
RESULT
Trace resistance
155.34 mΩ
MARGIN
to 160 mΩ
4.66 mΩ
→
→
→
→
LOT D risk drivers
Sulfur
5.0 > 4.0 ppm
+40
Conductivity
97.85 < 100.5 % IACS
+25
Resistance margin
4.66 mΩ < 10 mΩ
+15
PCN exception
17.8 ≥ 17.5 µm
+8
LOT D
88
HOLD
Chemistry + electrical + narrow resistance margin + documented exception
CU-JULY-2026-QUAL • 24 JUL 2026 • MODEL-DERIVED VISUAL READOUT
technical_findings_matrix.xlsx · Calculations!P5 → J21:L21 → O74:P74

## Slide 4
SENSITIVITY COMPARISONS
Same inputs. Only the stated scenario switch changes.
04
LOT D baseline 88 · HOLD
LOT B baseline 12 · CONDITIONAL
No oxygen waiver
LOT D
88 · HOLD
Δ +0
LOT B
44 · CONDITIONAL
Δ +32
B oxygen flips to FAIL; score rises 12 → 44.
No process change notice
LOT D
80 · HOLD
Δ -8
LOT B
12 · CONDITIONAL
Δ +0
D thickness flips to FAIL; exception points drop.
95 C service stress
LOT D
88 · HOLD
Δ +0
LOT B
12 · CONDITIONAL
Δ +0
D resistance flips to FAIL at 95 °C; score already carries margin flag.
Sensitivity does not create new evidence rows: it reuses the selected resistivity, assays, geometry, controlled limits, weights, and thresholds from Inputs.
CU-JULY-2026-QUAL • 24 JUL 2026 • MODEL-DERIVED VISUAL READOUT
technical_findings_matrix.xlsx · Scenarios!A4:AA7