Conductor Control Plan

| Field | Value |
| --- | --- |
| Document No. | CCP-CU-180 |
| Revision | 1.0 |
| Effective Date | 2026-05-20 |
| Author | Olivia Grant, Product Quality Engineer |
| Classification | Controlled |

## 1. Revision History

Rev. 1.0 supported pre-July pilot builds and remains available for traceability.

## 2. Electrical Acceptance

| Clause | Parameter | Value | Scope |
| --- | --- | --- | --- |
| E-1 | Minimum conductivity | 100.0 % IACS | all copper conductor lots |
| E-2 | Maximum trace resistance | 170 mOhm | 50 mm hybrid-bond verification trace |
| E-3 | Finished copper thickness floor | 17.0 um | hybrid-bond stack codes |

## 3. Qualification Note

Rev. 1.0 is not the governing electrical limit after the July supplier alignment notice.