Conductor Control Plan

| Field | Value |
| --- | --- |
| Document No. | CCP-CU-180 |
| Revision | 2.0 |
| Effective Date | 2026-07-01 |
| Author | Olivia Grant, Product Quality Engineer |
| Classification | Controlled |

## 1. Revision History

Rev. 2.0 tightens the electrical acceptance clauses for July production lots.

## 2. Electrical Acceptance

| Clause | Parameter | Value | Scope |
| --- | --- | --- | --- |
| E-1 | Minimum conductivity | 100.5 % IACS | all copper conductor lots |
| E-2 | Maximum trace resistance | 160 mOhm | 50 mm hybrid-bond verification trace |
| E-3 | Finished copper thickness floor | 18.0 um | hybrid-bond stack codes |

## 3. Supersession

Use Rev. 2.0 for clauses E-1 and E-2 for lots received on or after 2026-07-01. A later process change may supersede a narrower manufacturing parameter without changing the electrical limit.