Base Copper Conductor Material Limits

| Field | Value |
| --- | --- |
| Document No. | STD-CU-101 |
| Revision | 2.1 |
| Effective Date | 2026-06-18 |
| Author | Anika Rao, Materials Standards Lead |
| Classification | Controlled |

## 1. Purpose

Set the default chemistry acceptance ceilings for wrought and foil-grade copper used in conductor fabrication.

## 2. Applicability

Applies to July conductor lots unless a product-family standard or customer addendum states a narrower ceiling.

## 3. Limits

| Impurity or field | Limit / rule |
| --- | --- |
| Oxygen | 8.0 ppm |
| Sulfur | 8.0 ppm |
| Lead | 5.0 ppm |
| Bismuth | 3.0 ppm |
| Iron | 10.0 ppm |
| Nickel | 10.0 ppm |

## 4. Notes

The base table is retained as the broadest published reference; do not use it to relax a tighter applicable limit.