## Slide 1
July Copper Qualification Readout
source_register.xlsx -> technical_findings_matrix.xlsx -> qualification_readout.pptx -> risk_assessment.docx
13 material identities
2 held lots
1 conditional release
LOT-CU-2607-D top risk
Recommendation: release LOT-CU-2607-A and LOT-CU-2607-C; conditionally release LOT-CU-2607-B under MAT-WVR-26-071; hold LOT-CU-2607-D and LOT-CU-2607-E.
Grid: 0.45 in margins, 12-column rhythm, 0.25 in baseline. IDs, totals, and statuses match source_register.xlsx and technical_findings_matrix.xlsx.

## Slide 2
Source Coverage And Identity Resolution
Supplier/Lab
C10100, E-Cu58, HB electro-Cu, eta-tin copper
AFLOW
Ag-Al-Cu intermetallic top AUID aflow:aca47c434f9e2dc8
COD
Pure Cu F m -3 m / SG 225; oxides and Cu3Sn comparators
OQMD
Cu2O, CuO, Cu3Sn, Al-Cu, ZnCu, CuAu stability rows
PubChem/NIST
Copper identity support; sulfate and cuprate decoys rejected
Cu^1O resolves to Cu2O / cuprite, not CuO
Copper sulfate CID 24462 is identity-only, not OQMD stability
Grid: 0.45 in margins, 12-column rhythm, 0.25 in baseline. IDs, totals, and statuses match source_register.xlsx and technical_findings_matrix.xlsx.

## Slide 3
Resistance Margin And Scenario Sensitivity
Chart: 
| Governed 85 C | Room temp shortcut | Old Rev. 1 limit
Margin mOhm | 4.6557 | 36.264 | 14.6557
Governed resistance 155.34 mOhm
Margin to 160 mOhm 4.66 mOhm
Room-temp understatement 31.61 mOhm
Hold unchanged: sulfur + conductivity
Resistance chain: LR-COND-0726-06 rho=1.762 uOhm-cm; alpha=0.00393; temp=85 C; TRACE-HB-225 50 mm x 400 um; XR17 thickness=17.8 um; limit=160 mOhm.
Grid: 0.45 in margins, 12-column rhythm, 0.25 in baseline. IDs, totals, and statuses match source_register.xlsx and technical_findings_matrix.xlsx.

## Slide 4
Ranked Findings And Actions
RISK-01
LOT-CU-2607-D
80
Hold
Sulfur 5.0 ppm > 4.0; conductivity 97.85% IACS; 4.66 mOhm margin
RISK-02
LOT-CU-2607-E
40
Hold
Lead 5.4 ppm > 5.0 on intermetallic coupon
RISK-03
LOT-CU-2607-B
8
Conditional
Oxygen 6.2 ppm covered by MAT-WVR-26-071
Owner: Meredith Chen -> rerun sulfur and trace checks by 2026-07-13
Owner: Evan Brooks -> supplier lead RCA by 2026-07-12
Grid: 0.45 in margins, 12-column rhythm, 0.25 in baseline. IDs, totals, and statuses match source_register.xlsx and technical_findings_matrix.xlsx.