July Copper Conductor Qualification Risk Assessment

Audience: Manufacturing Quality Manager. Package dependency: source_register.xlsx -> technical_findings_matrix.xlsx -> qualification_readout.pptx -> risk_assessment.docx.

# 1. Summary

The July copper conductor refresh covers 13 in-scope material identities and five July release lots. The decision is to release LOT-CU-2607-A and LOT-CU-2607-C, conditionally release LOT-CU-2607-B under MAT-WVR-26-071, and hold LOT-CU-2607-D and LOT-CU-2607-E.

Top finding RISK-01 is LOT-CU-2607-D with score 80. The lot has sulfur above the 4.0 ppm customer limit, conductivity below 100.5% IACS, and a narrow trace-resistance margin of 4.66 mOhm.

| Lot | Decision | Risk score | Evidence basis |
| --- | --- | --- | --- |
| LOT-CU-2607-A | Release | 0 | Chemistry and conductivity pass |
| LOT-CU-2607-B | Conditional release | 8 | Oxygen covered by MAT-WVR-26-071; no other impurity waived |
| LOT-CU-2607-C | Release | 0 | Conductivity 100.90% IACS after calibration; chemistry pass |
| LOT-CU-2607-D | Hold | 80 | Sulfur 5.0 ppm > 4.0; conductivity 97.85% IACS; resistance 155.34 mOhm |
| LOT-CU-2607-E | Hold | 40 | Lead 5.4 ppm > 5.0 on eta Cu3Sn coupon |

# 2. Impact

The held lots block only the affected HB-RDL panel and BGA solder-interface coupon. Released lots remain available for standard conductor builds. Conditional release of LOT-CU-2607-B is limited to the annealed stitch-wire coupon and must not be generalized to other impurities or lots.

The governed resistance calculation for TRACE-HB-225 is 155.34 mOhm against a 160 mOhm limit. The room-temperature shortcut would understate resistance by 31.61 mOhm.

# 3. Timeline

| Timestamp | Event | Evidence |
| --- | --- | --- |
| 2026-07-02 09:18 PDT | HB service temperature set to 85 C for the July trace margin. | EMAIL-HB-WINDOW |
| 2026-07-03 13:42 PDT | Rev. 2 confirmed for E-1/E-2; PCN-HB-044 Rev. C limited to HB thickness floor. | EV-REV-01 |
| 2026-07-06 16:27 PDT | Nora Patel approved MAT-WVR-26-071 for LOT-CU-2607-B oxygen only. | EV-WVR-01 |
| 2026-07-08 21:14 UTC | XR-17 log recorded 17.8 um average copper thickness for LOT-CU-2607-D. | XR17-20260708-04 |
| 2026-07-09 05:12 UTC | Ingest log rejected broad literature metadata as property evidence. | LIT-0726-07 |

4. Contributing Factors

| Factor ID | Finding | Mechanism | Downstream effect |
| --- | --- | --- | --- |
| CI-01 | Customer sulfur limit | CQA-CU-772 sets sulfur at 4.0 ppm, below the published 6.0-8.0 ppm limits. | LOT-CU-2607-D becomes a hold. |
| CI-02 | Temperature-adjusted resistance | Resistivity, temperature coefficient, service temperature, geometry, and thickness combine to produce a narrow margin. | Resistance is watch-banded even before chemistry hold. |
| CI-03 | Oxygen waiver | MAT-WVR-26-071 applies only to LOT-CU-2607-B oxygen up to 7.0 ppm. | Lot B is conditional release, not hold. |
| DQ-01 | Duplicate sync rows | Duplicate lab rows are retained as evidence but not counted twice. | Violation count remains two held lots. |
| DQ-02 | Catalog decoys | PubChem canonicalization and broad literature metadata are identity/context evidence, not stability/property proof. | Copper sulfate and YBCO are excluded from release conclusions. |

# 5. Response

The technical model uses the 13-row material population from the source register, Rev. 2 electrical criteria, PCN-HB-044 Rev. C for HB thickness, strict impurity limits, measured-value priority, and condition-matched property values.

Measured property priority is applied directly: MAT-CU-C101 uses 101.52% IACS rather than the nearby 101.0% literature value, MAT-CU-HBPLATE uses 219 MPa yield strength under 23 C / 101.3 kPa / 1E-3 s^-1 rather than the 176 MPa accelerated condition, and thermal conductivity uses measured values of 392.6 W/mK and 386.8 W/mK for MAT-CU-C101 and MAT-CU-HBPLATE respectively.

The AFLOW intermetallic screen ranks aflow:aca47c434f9e2dc8 first at -0.0973103 eV/atom, followed by aflow:53725bf233e77afc at -0.0961982 eV/atom and aflow:65ad75192503ef40 at -0.0915473 eV/atom.

Catalog reconciliation keeps MAT-CU2O-CUPRITE as Cu2O from legacy Cu^1O notation, separates it from MAT-CUO-TENORITE, and rejects copper sulfate CID 24462 as identity-only because no OQMD sulfate stability row is present.

The readout carries the same top-three ranking: LOT-CU-2607-D score 80 hold, LOT-CU-2607-E score 40 hold, and LOT-CU-2607-B score 8 conditional release.

6. Corrective Actions

| Action ID | Owner | Due | Closure criteria | Linked risk |
| --- | --- | --- | --- | --- |
| CA-01 | Meredith Chen | 2026-07-13 | Repeat sulfur assay and TRACE-HB-225 resistance on replacement HB-RDL panel; release only if sulfur <= 4.0 ppm and margin remains positive. | RISK-01 |
| CA-02 | Evan Brooks | 2026-07-12 | Quarantine LOT-CU-2607-E coupon and obtain supplier lead-contamination RCA with corrected COA. | RISK-02 |
| CA-03 | Nora Patel | 2026-07-14 | Attach MAT-WVR-26-071 to the release record and verify next E-Cu58 oxygen result is <= 5.0 ppm. | RISK-03 |
| CA-04 | Omar Shah | 2026-07-15 | Mark LIT-0726-07 and MAT-YBCO-CUPRATE as decoys in the source register for future runs. | DQ-02 |

7. Evidence Cross-Reference

| Claim | Primary evidence | Second evidence | Output dependency |
| --- | --- | --- | --- |
| Sulfur breach | ASSAY-0726-04 | CQA-CU-772 | source register -> model -> readout -> review |
| Oxygen exception | ASSAY-0726-02 | MAT-WVR-26-071, Nora Patel, 2026-07-06 | source register -> model -> review |
| Resistance margin | LR-COND-0726-06 and TRACE-HB-225 | CFG-QA-CU-0726, XR17 log, CCP-CU-180 Rev. 2 | model -> readout -> review |
| AFLOW intermetallic | aflow:aca47c434f9e2dc8 | Ag1Al1Cu1 formation enthalpy -0.0973103 eV/atom | source register -> model |
| PubChem/OQMD exclusion | CID 24462 CuO4S | No OQMD sulfate row | source register -> model -> review |